Technical Data Sheet

Product Name:		Industrial Flooring Epoxy

Description:			Two-Component Epoxy

Chemistry:			Mixed Polyamines and Bisphenol A Resin

Color:				Gardener 1-2

Viscosity:			@ 25 c. 3300 Centipoise

Refractive Index:		Approx 1.48

Tensil Strength:		3,450- 3,550 PSI

Flexibility:			½” Mandrel Bend, No Cracking or Adhesion Failure

Chemical Resistance:	Excellent Resistance to Aliphatic and Aromatic Hydrocarbons Salts, Acids and Alcohols

Physical Testing:		Pencil Hardness		4-5H

Salt Spray			200 Hrs. Min.

QUV (Xenon Bulb)		500 Hrs. Min.

Falling Sand Test		28 Liters Min.

Cross Hatch			100%

Gardner Impact:

Reverse			140Lbs.

Forward			140 Lbs

Testing Done on Cured 2-Mil. Coating on Aluminum Q-Panels, Aged Seven (7) Days.

Shelf Life:	12 Months In Orginal Unopened Pails, Stored at Room Temperature

Recommended Equipment For Application and Curing

Equipment: Brush, Roll (Short Nap) or Spray With Professional HVLP

This Statement is Made in Liew of All Warranties Express or Implied.  Slide-Lok Guarantees Products of its Manufacture to be Free From Defects in Workmanship and Materials For A Period of Three (3) Months From The Date Of Shipment To Original Purchaser.  Manufacturers Only Obligation Shall Be To Replace Such Quantity Proved To Be Defective And Shall Not Be Liable For Injury, Loss Or Damages Direct Or Consequential Arising Out Of Use Or The Inability To Use This Product. Before Use, User Shall Determine Suitability Of Product For Their Intended Use.  User Assumes All Risks And Liability In Connection Herewith.