Slide-Lok’s solid color floor system.

Mixing ratio is 1 part A to 1 part B. Kits come in 6 gallons, 3 gallons part A and 3 gallons part B.

The mixing ratios are as follows:  You will likely mix in smaller amounts, especially for cut-in, just keep the ratios in proportion:

Mixing- Prime Coat

- 64 ounces of part A

- 8 ounces of Pigment

- Mix together

- 64 ounces of part B

- 25 ounces of Acetone

- Mix all together with stir stick back and forth for 2 minutes. Remember to scrape the sides and the bottom of the mixing bucket.

1 gallon of product cut back 20% for prime coat – you should see coverage rates of around 250 sq. ft / gallon

Mixing- Chip Coat

- 64 ounces of part A

- 8 ounces of Pigment

- Mix together

- 64 ounces of part B

- 16 ounces of Acetone

- Mix all together with stir stick back and forth for 2 minutes. Remember to scrape the sides and the bottom of the mixing bucket.

1 gallon of product cut back 12% to 15% for your chip coat – you should see coverage rates of around 400 sq. ft / gallon

Mixing- Top Coat

- 64 ounces of part B

- 64 ounces of part A

- 4 ounces of Acetone

- Mix all together with stir stick back and forth for 2 minutes. Remember to scrape the sides and the bottom of the mixing bucket.

1 gallon of product cut back 12% to 15% for your top coat – you should see coverage rates of around 250 sq. ft / gallon.

If you do a 2nd top coat, do a thin coat, keep the coverage rate to around 400 sq. ft / gallon.

Floor chips – full chip floor.  Throw approx. 1 lb per 6 sq. ft.  You should recover 35% - 50% of what you throw.